## Slide 1: Ultrafast laser based 3D printing of photonic structures Robert R. Thomson Scottish Universities Physics Alliance (SUPA), Institute of Photonics and Quantum Sciences (IPaQS), Heriot-Watt University, Edinburgh, UK.

## Slide 2
Ultrafast laser inscription (ULI)

## Slide 3
Bellouard et. al., Opt. Express. 12, 2120 (2004)
Little et. al., Opt. Express. 16, 20029 (2008)
Refractive index modification
Chemical etch-rate modification
Ultrafast laser induced modifications

## Slide 4
3D integrated waveguide fan-outs

## Slide 5
Photonic-enabled
precision spectrographs
Lab throughput ~ 70% for incoherent multimode light @ 1550 nm.
“Appears” not to induce modal noise.

## Slide 6
z
y
x

## Slide 7
z
y
x

## Slide 8
z
y
x

## Slide 9
60 µm
Transmission mode microscope image through a ULI fabricated volume grating in gallium lanthanum sulphide chalcogenide glass.

## Slide 11
Coated Uncoated
(b)
Anti-reflection coating GLS

## Slide 12
Ultrafast laser induced selective etching
Bellouard et. al., Opt. Express. 12, 2120 (2004)
High aspect ratio surface -channels
Bellouard et. al., Opt. Express. 13, 6635 (2005)
Bellouard et. al., Opt. Express. 12, 2120 (2004)
Sub-surface -channels
-mechanics

## Slide 13
Yves Bellouard,
Opt. Express 13, 6635-6644 (2005)

## Slide 14
Yves Bellouard,
Opt. Express 13, 6635-6644 (2005)

## Slide 15
Yves Bellouard,
Opt. Express 13, 6635-6644 (2005)

## Slide 18
90% and 99% survival stresses are ~200 N.mm−2 and ~70 N.mm−2
Adhesives exhibit failure strengths of ∼10 to 20 N.mm−2.
Weibull plot for borosilicate - borosilicate

## Slide 19
David Hélie et al, Opt. Mater. Express 3, 1742-1754 (2013)

## Slide 20
Freeform silica micro-optics (and possibly even macro-optics)
Freeform silica microlens IFU’s with PA slots for optical fibres
Freeform volume gratings (visible-to-mid-IR) - integrated into optics
Low-cost, high volume precision encoders for position sensing
Ultrafast laser welding of fibres to dielectrics and metals
(avoid issues with gluing e.g. cryogenics)
Possible applications?
The case:
High risk / high reward research: enabling & potentially revolutionary
Excellent commercialisation and spin-out opportunities
Solution looking for problems: Now is the time to exploit the capabilities of ultrafast laser printing